Pure Heat Conduction, Multizone and Isothermal Case

written by Josep M. Vilarrasa Díaz

Institut für Metallurgie, TU-Clausthal

The improvement of the solidification processes is very interesting for the Metallurgical Industry due to its high cost and difficulty. Each year they invert huge amounts of money to investigate in this field. That’s the reason why in the last years the use of computers to simulate the processes have become very important, letting the companies reduce the number of the expensive experiments to test new methods or materials. Thanks to the high accuracy of the power simulation computer tools is possible to investigate in laboratories without wasting energy (i.e., energy needed to melt metals), leading to a reduction of the costs for the company and saving energy for the environment.

September 15th, 2003

| Contents |  |
| --- | --- |
| Introduction | 2 |
| Program description | 2 |
| Problem description | 2 |
| Calculations | 4 |
| 4.1 Equations solved …………………………………………………………..... | 4 |
| 4.2 Calculations for Aluminium ………………………………………………... | 4 |
| 4.3 Calculations for Iron ………………………………………………………... | 6 |
| How were these diagrams obtained? | 9 |
| Summary and conclusions | 9 |
| References | 10 |

# Introduction

Several decades ago it was quite difficult to predict what was going on when a metal solidifies. Nowadays and thanks to the high calculation capacity of computers we can simulate with a high accuracy the solidification process of metals.

In particular this simulation has been done by using CFD-ACE+, a computational fluid dynamics program which has very powerful simulation tools.

# Program description

CFD-ACE+ is a set of computer programs for multi-physics computational analysis. The programs provide an integrated geometry and grid generation module (CFD-GEOM), a graphical user interface for preparation of the model (CFD-GUI), a computational solver for performing the simulation (CFD-ACE(U)), and an interactive visualization program for examination and analysis of the simulation results (CFD-VIEW).

The program has many different modules for each type of calculation (flow, heat, turbulence, radiation…), being possible to use different modules at the same time. The ability to perform heat transfer analysis is an integral part of the CFD-ACE(U) solver. The program can be used to simulate many types of heat transfer problems. The simplest are pure heat conduction problems (this case). More advanced applications will add the simulation of flow. Ultimately the Heat Transfer Module solves for the energy in the system and can therefore be used to produce the temperature field energy transfer characteristics of the model.

# Problem description

We have simulated the solidification process of a 2D box with two different metals, Aluminium and Iron in order to compare the differences between these two materials. The box has the following properties:

- Square 10x10 cm.

- Top and right walls are Isothermal (T=363°K). Wall width = 1 cm.

- Crucible material: Aluminia (Al2O3). Physical properties of the material needed for the simulation (Data given by Morgan Advanced Ceramics):

|  | Value | Units |
| --- | --- | --- |
| Density | 3850 | kg/m3 |
| Specific Heat | 900 | J/(kg*K) |
| Heat Conductivity | 25 | W/(m*K) |

- Bottom and left walls are Adiabatic (heat transfer = 0).

As we will see below, Iron and Aluminium have very different physical properties values so it’s quite difficult to compare them when, for example, Aluminium has a melting temperature of 933,25°K and for Iron is 1808°K. What I had done is equalize the heat quantity the metals have to remove during the solidification. So we have the following:

| where, | m: mass [kg] |
| --- | --- |
|  | Cp: specific heat at 293°K V: volume |
|  | δ: density |
|  | T0: initial temperature |
|  | TS: solidification temperature |

Now we can simplify the equation setting ∆T for Iron in 100° (so T0 for Fe will be 1908°K) and we also know that the volume is always the same. We substitute the variables for the values:

So the simulation for the solidification process will start at 1908°K and 1092°K for Fe and Al, respectively. The two metals will transfer the same heat quantity and we will be able to compare them and see how much influence the other physical parameters such as the specific heat or the thermal conductivity in the solidification.

# Calculations

4.1	Equations solved

Here I describe the mathematical equations used by CFD-ACE(U) and its Heat Transfer Module. Heat transfer processes are computed by solving the equation for the conservation of energy. This equation can take several forms and CFD-ACE(U) numerically solves the energy equation in the form known as the total enthalpy equation. This form is fully conservative and is given in the next equation.

4.2	Calculations for Aluminium

First of all we describe the physical properties of Al needed for the simulation. In order to get a more realistic solution, CFD-ACE(U) lets the user to introduce the required inputs in different ways. We had used the next evaluation methods: Constant, for constant values, and Piecewise Linear in T, linear interpolation of specified variable versus T data.

(for more details, look at Q:\agspitz\cfdrc\Mia\Aluminium data)

Required input values:

| Density: 2702 kg/m3 |
| --- |
| Latent heat: 399903 J/kg |
| Solidification temperature: 933,25 °K (660,25 °C) |
| Initial temperature of the solidification zone: 1092°K |
| Temperature of isothermal Aluminia walls: 363°K |
| Specific Heat: Temp [°K] Cp [J/(kg*K)] 273 885 933,25 1235 933,35 1090 1193 1090 Specific heat vs. temperature diagram→ |  |
| Viscosity (dynamic): Temp [°K] ν [kg/(m*s)] 933.25 1.25103633 1000 1.08549099 1200 0.77980016 1400 0.61571715 1600 0.51573867 1800 0.44934353 2000 0.40243665 Viscosity vs. temperature diagram→ |  |
| Thermal conductivity: Temp [°K] Tc[W/(m*K)] 303 235.8846 933,25 226.91396 933,35 100.13612 1293 117.8072 Thermal conductivity vs. temperature diagram→ |  |

Another very important thing are the numerical parameters used to solve the simulation. The table below shows which ones I had used:

| SOLVER CONTROLS |  |  |  |  |
| --- | --- | --- | --- | --- |
| Iter | Shared | Max. Iterations | 1000 |  |  |
|  |  | Convergence Crit. | 0.00001 |  |  |
|  |  | Min. Residual | 1E-18 |  |  |
| Spatial | Spatial Differencing | Enthalpy | Upwind |  |  |
| Solvers | Solvers | Enthalpy | CGS+Pre | 2500 | 0.00001 |
| Relax | Inertial Relaxation | Enthalpy | 0.5 |  |  |
|  | Linear Relaxation | Temperature | 0.2 |  |  |
| Limits |  | Enthalpy | -1E+20 | 1E+20 |  |
|  |  | Temperature | 1E-10 | 5000 |  |
| Adv | Heat transfer | CFL Relaxation | Disabled |  |  |

For more information about the input numerical parameters, please look at CFD-ACE(U) User Manual – Chapter 12: Numerical Parameters.

After the simulation, I obtained the following results:

The way I had obtained this diagram and the conclusions of the simulation are explained below. (for more details and information about the diagram and the data, look at Q:\agspitz\cfdrc\Mia\Case\Al+Aluminia crucible)

4.3	Calculations for Iron

Here I’m doing the same as I had done with the Aluminium calculations. I entered all these physical properties of the material:

(for more information, look at Q:\agspitz\cfdrc\Mia\Steel and Iron data)

Required input values:

| Density: 7874 kg/m3 |
| --- |
| Latent heat: 530769.23 J/kg |
| Solidification temperature: 1808 °K (1535 °C) |
| Initial temperature of solidification zone: 2000 °K (1827 °C) |
| Temperature of isothermal Aluminia walls: 363°K |
| Specific heat: Temp [°K] Cp [J/(kg*K)] 273 480 323 500 473 550 573 595 673 650 773 720 873 900 933 1140 1043 1140 1063 930 1173 850 1193 650 1603 750 1808 770 2273 770 | Specific heat vs. temperature diagram |
| Viscosity: Temp [°K] v [kg/(m*s)] 1808 0.0074087 1830.41 0.00665226 1875.11 0.00615849 1938.84 0.00576669 1988.97 0.00557522 2129.21 0.00522546 Viscosity vs. temperature diagram→ |  |
| Thermal conductivity: Temp [°K] Tc[W/(m*K)] 303 80 373 72 473 64 673 51 853 40 1063 29 1193 29.5 1198 27 1473 31.5 1808 33.5 1808.1 35 2273 35 | Thermal conductivity vs. temperature diagram |

Another very important thing are the numerical parameters used to solve the simulation for Iron. The table below shows which ones I had used:

| SOLVER CONTROLS |  |  |  |  |
| --- | --- | --- | --- | --- |
| Iter | Shared | Max. Iterations | 1000 |  |  |
|  |  | Convergence Crit. | 0.00001 |  |  |
|  |  | Min. Residual | 1E-18 |  |  |
| Spatial | Spatial Differencing | Enthalpy | Upwind |  |  |
| Solvers | Solvers | Enthalpy | CGS+Pre | 2500 | 0.00001 |
| Relax | Inertial Relaxation | Enthalpy | 0.5 |  |  |
|  | Linear Relaxation | Temperature | 0.2 |  |  |
| Limits |  | Enthalpy | -1E+20 | 1E+20 |  |
|  |  | Temperature | 1E-10 | 5000 |  |
| Adv | Heat transfer | CFL Relaxation | Disabled |  |  |

For more information about the input numerical parameters, please look at CFD-ACE(U) User Manual – Chapter 12: Numerical Parameters.

After the simulation, I obtained the following results:

The way I had obtained this diagram and the conclusions of the simulation are explained below. (for more details and information about the diagram and the data, look at Q:\agspitz\cfdrc\Mia\Case\Iron+Aluminia crucible).

# How were these diagrams obtained?

Using the CFD-VIEW program it’s possible to get all the values and diagrams needed. Using the animation simulation tools and the plot function it’s easier to see and understand the whole solidification process.

The diagrams are showing the position of the solid fraction front in each point of the box (see attached picture with the red spots) against time, so we can realize how fast solidifies the metal in each point of the solidification zone. xs=1 means the metal have already solidified and xs=0 it’s when the metal starts to solidify. It’s also a good reference to study when xs=0.5.

# Summary and conclusions

The aim of this report is to compare the solidification process for Aluminium and Iron. Due to their different physical properties I had to describe a method which allows to compare the two metals so they have to carry out the same amount of energy by conduction. The equation used was the following: (I set the ∆T for Iron to 100°)

The results are the diagrams above. In order to realize the differences, I also show the comparison between the two diagrams with a solid fraction of xs=0,5:

We can realize that the box with iron needs more time to solidify due to its worse thermal conductivity and specific heat values. The values of thermal conductivity for iron are lower than Al values, so Fe can’t conduct heat as well as Al. And also the value of latent heat for iron is higher so Fe contains more heat (Joules) per kg.

The sum of all these factors play against the speed of solidification of Iron, concluding that Al can carry out faster the overall energy to solidify by conduction.

# References

- Handbook of Chemistry and Physics, by Chemical Rubber Co. 50th Edition

- Physikalische Stoffeigenschaften der reinen Metalle, VSI-Handbuch Betriebstechnik

- The Viscosity of Liquid Iron and Iron-Carbon Alloys, by R. N. Barfield and J. A.

Kitchener, published in Journal of the Iron and Steel Institute, August 1955.

- CFD-ACE(U) User Manual, Version 2002 by CFD Research Corporation.

- CFD-ACE(U) Modules, Version 2002 by CFD Research Corporation.

# Footnotes

miavilarrasa@vodafone.es

http://www.imet.tu-clausthal.de